Groundbreaker Mk3     Technical Data:

Size 				500 x 330 x 170 mm

Connections 			Philmac / Protecta-line type taking

25mm Dia MDPE

MDPE barrier pipe systems

Various butylised rubber pipes

Plastic covered copper*

32mm dia MDPE*			* requires adaptor

Control valve			Standard washer / spindle

NRV				Watts Ocean

Shell				Injection moulded in 90% recycled polypropylene

UV Stabilised

Impact resistant

50+ year design life

Insulation          			Thermal conductivity 	< 0.025 W/mK

Water absorption 	< 0.1% by volume

Exceeds WIS 4-37-01 	(no freezing after 5 days at -150C)

Pressure Rating 		QA Certified to12 bar 	(Tested to 16 bar)

Flow Rate			As feed pipe

[25mm dia = 0.6m3/hr; 32mm dia = 1.0m3/hr under “normal” pressures]

Water meter compatible type 	All concentric types

Tools required			Drill, 7mm masonry bit, screwdriver (Philips type)

Packaging 			Shrink-wrapped film

Fitting instructions		Enclosed within shrink-wrap

Fixing kit	Wall plugs, screws, washers, pipe inserts etc. inside shrink wrapped unit

Shelf Life			Indefinite

Storage Requirements		No special requirements (indoor or outdoor)

Carriage Requirements		No special requirements

Additional features

Compliant with “Secure by Design” criteria

Compliant with Building Regulations Part M

Within PPG3 Planning Guidelines

Compliant with Radon alleviation designs

Ideal for use on Brownfield redevelopment sites / contaminated land

Ideal for lead & water service replacements without excavation

Adaptor available for		Link to ¾ inch BSP thread (standard plumbing fitting)

Allows connections to hosepipes etc.

Water control easily available above ground

Water control at the point of delivery

Ideal for independent water management

Landlords supply

Bib Tap housing